Fresco

Composition		85% PVC, 15% Polyester

Width			137cm

Thickness:		1.0mm

Weight		849.4 grams per lineal meter

Abrasion		Heavy Duty Commercial, 50,000+ Martindale

Flammability		AS 3744.1, IMO 652(16), AS1530.3

Qualities	Heavy duty commercial vinyl with a soil resistant finish together with UV stabilisers & antimicrobial finish. The antimicrobial properties inhibit the growth of mould, mildew or bacteria. This high spec vinyl is suitable for marine, healthcare and all heavy duty commercial environments.

Care Instructions

- Prompt cleaning recommended.

- Ordinary dirt and stains can be removed with mild soap and water. E.g. Sards soap.

- 1:10 bleach solution can be used if the vinyl is rinsed well after this process. Please note, excessive amounts of bleach, or not rinsing thoroughly, will have a negative effect on the vinyl.

- Vinyl can be cleaned with leather cleaner.